## Slide 1
Primary funding is provided by
The SPE Foundation through member donations
and a contribution from Offshore Europe
The Society is grateful to those companies that allow their professionals to serve as lecturers
Additional support provided by AIME
Society of Petroleum Engineers Distinguished Lecturer Program
www.spe.org/dl

## Slide 2
Cement Testing
Are We Looking at The Right Things The Wrong Way?
Don Purvis
Marathon Oil Company
Society of Petroleum Engineers Distinguished Lecturer Program
www.spe.org/dl

## Slide 3: A Brief History of Oil well Cement Testing
“Cements for Oil Wells, Status of Testing Methods and Summary of Properties”; W W Robinson, May 1939
First Official Document : “API Code for Testing Cements Used in Wells”; Code 32*, February 1948
*Code 32 Evolved into current ISO-10426 / API Spec 10A

## Slide 4: Code 32 Testing Included:
Cement Sampling
Slurry Fluidity (Correct water content)
Thickening Time Test
Consistometer Test
Tensile –Strength Test
Foam Test

## Slide 5: Let’s Talk About Three of Those Tests
Thickening Time Test
Consistometer Test
Tensile –Strength Test

## Slide 6: Thickening Time Test
First Described in Code 32
“Cement for Oil Wells: Status of Testing methods & Summary of Properties”
W.W. Robinson May 1939
First Test made with Ice Cream Freezer & Electric Heater Otis D. Small ……. 1929
May 1939
1929

## Slide 7: The Jet Mixer Patented in 1921

## Slide 8: Modern Cement Pump in the Early 40’s

## Slide 9: Cement Complexity & Code 32
Code 32 Designed for ‘Neat’ Cement
1951 Francis Anderson (Halliburton) Review of Developments Code 32
  “Casing cementing only”
  “Impossible to test cement slurries containing some of the present day additives”

## Slide 10
1939 Thickening Time Tester
Cement for Oil Wells: Status of Testing Methods and Summary of Properties
W.W. Robinson; May 17, 1939

## Slide 11
1939 Cement Consistometer
Cement for Oil Wells: Status of Testing Methods and Summary of Properties
W.W. Robinson; May 17, 1939

## Slide 12
Slurry Density
Thickening Time
Compressive Strength
Fluid Loss
Rheology / Gel Strength
Stability / Free Fluid
Compatibility
Seven Standard tests Outlined in ISO 10426-1:
Where Are We Today?
And Then ……….

## Slide 13: API-65-2 Published December 2010
…..In his expert report, Glen Benge concluded that cement didn't cut off the flow of hydrocarbons into the well because of inadequate design of the cementing slurry…….
Macondo April 21, 2010
…”based mainly on experiences in the United States outer continental shelf”…..

## Slide 14
Seven Standard tests Outlined in ISO 10426-1:
Let’s Examine Three of These:
Where Are We Today?
Slurry Density
Thickening Time
Compressive Strength
Fluid Loss
Rheology / Gel Strength
Stability / Free Fluid
Compatibility
Static Gel Strength
Shrinkage/Expansion
Sheath Integrity
Three Additional in RP 65-2:
Slurry Density
Thickening Time
Compressive Strength
Fluid Loss
Rheology / Gel Strength
Stability / Free Fluid
Compatibility
Static Gel Strength
Shrinkage/Expansion
Sheath Integrity

## Slide 15: ‘Thickening Time’ We Have Come a Long Ways
Consistometer Then & Now
Circa 1939
Circa 2014

## Slide 16: Consistometers Then and Now
 | 1939 | 2014
Maximum Temperature | 180 deg F | 600 deg F
Mixing process | Slurry Jar | Precision Blender
Blends Tested | Cement & Water | Complex Systems & Additives
Measurement | Pendulum & cord | High Temp Spring & Rheometer
Stirring Device | Modified ice cream paddle | Modified Ice Cream paddle

## Slide 17: Or Have We?......
Consistometer Chamber Then & Now
1939
2014

## Slide 18: Consistometers Is There a Better Way?

## Slide 19: Stirring Shear Rate: What Difference Does it Make?
Slurry Blend | Temp | Thickening Time |  | Delta
API Class plus additives | ⁰F | API Paddle @ 150 RPM | Helical Screw @ Actual Shear | 
G + 2% CaCl | 75⁰ | 4:10 | 2:25 | 72%
35:65:6 Poz:C:Gel + 5% NaCl | 75⁰ | 8:10 | 6:00 | 36%
H + 3% SMS | 90⁰ | 7:40 | 1:35 | 480%
G +35%SF +1%FLA +1.2%LSR 15.8 ppg | 197⁰ | 3:10 | 4:40 | 32%
H +35%SF +1.5%HTFLA + 0.6% SR 16.2 ppg | 308⁰ | 3:15 | 5:00 | 35%

## Slide 20: Compressive/ Tensile Strength
Early Tests were Tensile
Cement for Oil Wells: Status of Testing Methods and Summary of Properties
W.W. Robinson; May 17, 1939

## Slide 21: Tensile Strength Lost Favor
Very Difficult to Cure /Cool/ Remove & Test

## Slide 22: Replaced with Compressive
Simpler, more consistent, could be modeled with a UCA

## Slide 23: Unfortunately:
Wellbore Cement Fails in Tension
Tensile Tests Are Not Specified in ISO-10426 or API RP 10B-2

## Slide 24: Today’s Tensile Testing ‘TBDC’ Test
CAM
Test Performed under Temperature and Pressure

## Slide 25: Today’s Tensile Testing Brazilian Test
CAM

## Slide 26: Conclusion
Do not rely on standard tests
We have the technology to test the Right Things The Right Way
If your wellbore integrity is important:
Consider going beyond ISO/ API
Understand what you expect your cement to do
Test accordingly

## Slide 27
Society of Petroleum Engineers Distinguished Lecturer Program
www.spe.org/dl
Your Feedback is Important
Enter your section in the DL Evaluation Contest by completing the evaluation form for this presentation :
Click on: Section Evaluation